Certificate of Analysis

Hydroxypropyl Methyl Cellulose(HPMC, Pharmaceutical Grade) (200520-E-15)

BATCH NUMBER        20191011                 TEST DATE            10-11-2019

QUANTITY (kg)          1000        	         MANUFACTURE DATE     10-10-2019

PACKING             25kg/drum                EXPIRATION DATE      10-09-2021

| TEST | SPECIFICATION | RESULT |
| --- | --- | --- |
| Appearance | White or off-white powder ,no visible evidence of contamination by foreign matter | Conforms |
| Identification | Conform | Conforms |
| pH | 4.0-8.0 | pH6.0 |
| Viscosity | 12-18mPa.s | 15.5mPa.s |
| Water-insoluble | Not More Than 0.5% | 0.40% |
| Loss on drying | Not More Than 5.0% | 3.91% |
| Residue on ignition | Not More Than 1.5% | 1.27% |
| Heavy Metal | Not More Than 0.002% | ＜0.002% |
| Arsenic | Not More Than 0.0002% | ＜0.0002% |
| Methoxy | 28.0% to 30.0%CH3O Calculated on the anhydrous basis | 29.71% |
| Hydroxypropoxy | 7.0% to 12.0% C3H7O2 Calculated on the anhydrous basis | 8.32% |
| Bioburden |  |  |
| Total Microbial Count | Not More Than 1000CFU/gram | 350CFU/gram |
| Total Mold and Yeast | Not More Than 100CFU/gram | 30CFU/gram |
| Escherichia Coli | Negative | Not Detected |