Certificate of Analysis

63s Bioglass(63%SiO2+31%CaO+6%P2O5, >99%, <20μm)(214982)

| TESTS Appearance Purity % Avg particle size (μm) Total Heavy metals (mg/kg) Pb Hg As Cd | SPECIFICATIONS White powder ≥98 0 ~ 40 ≤50 ≤30 ≤5.0 ≤3.0 ≤5.0 | RESULTS Conforms 99.4 18.5 <10 <5 <2 <1 <2 |
| --- | --- | --- |