Certificate of Analysis

45s Bioglass(Actimins, 45%SiO2+24.5%Na2O+24.5%CaO+6%P2O5, >98%, 30µm) (610982)

| Product name | 45s5 bioglass (Actimins) |
| --- | --- |
| Production date | May. 25, 2016 | Product type | 45s5BG-D2 |
| Expiry date | May. 24, 2019 | Quantity | 1000G |

| TESTS Appearance Purity % Avg particle size ( μm ) Total Heavy metals ( mg/kg) Pb Hg As Cd | SPECIFICATIONS White powder ≥98 0 ~ 78 ≤50 ≤30 ≤5.0 ≤3.0 ≤5.0 | RESULTS Conforms 99 30 <20 <10 <3 <2 <2 |
| --- | --- | --- |

Please store product in cool and dry place, protected from light and keep the product hermetical in package while not in use.